STANDARD OPERATING PROCEDURE

Speckle-based Digital Image Correlation (DIC)

Using MATLAB — From Image Acquisition to Strain Maps

GRISHMA Undergraduate Summer Research Program

KRITI Initiative | IIT Kharagpur

Materials Science Center

Faculty: Prof. Shibayan Roy

Project Reference: GRISHMA-FAC-2026-0140

MATLAB R2026a | Image Processing Toolbox

Version 1.0 | June 2026

# 1. Overview and Purpose

This Standard Operating Procedure (SOP) describes the complete workflow for performing Speckle-based Digital Image Correlation (DIC) analysis using MATLAB. It covers the entire process from capturing images during a tensile test to obtaining full-field displacement and strain maps.

DIC is a non-contact optical technique that tracks the movement of a random speckle pattern applied to the surface of a specimen. By comparing images captured at different stages of deformation, the full displacement and strain field across the specimen surface can be computed.

## 1.1 What This SOP Covers

- Specimen preparation and speckle pattern application

- Camera and test machine setup

- Image acquisition during tensile testing

- MATLAB environment setup

- Running the DIC analysis code

- Interpreting the output results

- Validating the results

- Common errors and troubleshooting

## 1.2 Required Software

| Software | Version | Required Toolboxes |
| --- | --- | --- |
| MATLAB Online | R2026a or later | Image Processing Toolbox |
| MATLAB Online | R2026a or later | Statistics and Machine Learning Toolbox |
| MATLAB Online | R2026a or later | Parallel Computing Toolbox (optional, for speed) |
| Web Browser | Any modern browser | For MATLAB Online access |

⚠ NOTE: MATLAB Online is accessible at matlab.mathworks.com using your institutional login. All required toolboxes are included in the standard academic license.

# 2. Specimen Preparation

## 2.1 Speckle Pattern Application

The quality of the speckle pattern is the most critical factor in DIC accuracy. A poor speckle pattern will produce noisy, unreliable results regardless of how good the algorithm is.

### 2.1.1 Materials Required

- White spray paint (matte finish)

- Black spray paint (matte finish)

- Sandpaper (400–600 grit) for surface preparation

- Isopropanol / acetone for cleaning

- Masking tape to protect grip areas

### 2.1.2 Step-by-Step Application

- Clean the specimen surface thoroughly with isopropanol. Remove all oil, dust, and oxidation.

- Lightly sand the gauge section surface to improve paint adhesion. Wipe clean again.

- Apply a thin, uniform white base coat. Allow to dry completely (15–20 minutes).

- Apply black speckles by spraying briefly from a distance of 30–40 cm. The goal is random black dots.

- Check speckle size — individual dots should be 3–5 pixels in the captured images.

- Allow paint to cure for at least 30 minutes before testing.

### 2.1.3 Good vs Bad Speckle Pattern

| Property | Good Pattern | Bad Pattern |
| --- | --- | --- |
| Speckle size | 3–5 pixels in image | Too large (>10px) or too small (<2px) |
| Coverage | 40–60% black, 40–60% white | Too dense (>70% black) or too sparse (<20%) |
| Distribution | Random, uniform across gauge | Clustered or periodic pattern |
| Contrast | High contrast black on white | Low contrast, grey tones |
| Edge definition | Sharp, clear edges | Blurry, soft edges |

⚠ NOTE: Never use glossy paint. Specular reflections will corrupt the correlation. Always use matte finish paint.

# 3. Experimental Setup

## 3.1 Camera Setup

- Mount the camera on a rigid stand perpendicular to the specimen surface. Any out-of-plane tilt introduces error in the strain measurement.

- Set the camera as close as possible to fill the frame with the gauge section. The speckle region should occupy at least 50% of the image width.

- Use a fixed focal length lens. Never use autofocus during the test — it changes the magnification between frames.

- Set ISO as low as possible (100–400) to minimize noise. Use a fast shutter speed (1/500s or faster) to avoid motion blur.

- Use remote shutter release or intervalometer to avoid camera shake during image capture.

- Set white balance manually. Auto white balance can change colour temperature between frames.

## 3.2 Lighting Setup

- Use diffuse, uniform lighting. Avoid direct flash or specular highlights on the specimen.

- LED panel lights positioned at 45° to the specimen work well.

- Ensure lighting does not change during the test — do not use windows or variable light sources.

## 3.3 Alignment Check

Before starting the test, capture one image and verify:

- The gauge section is clearly visible and fills a good portion of the frame.

- Speckle dots are sharp and in focus.

- No specular reflections or shadows on the gauge section.

- Camera is level — the specimen axis should be horizontal or vertical in the image.

⚠ NOTE: Take a test image before mounting the specimen. Check that the speckle pattern is visible and well-contrasted at the planned camera position.

## 3.4 Image Acquisition During Testing

- Set the testing machine to capture images at regular displacement or load intervals.

- Recommended: capture one image every 0.05–0.1 mm of crosshead displacement for metals.

- Name images sequentially: img01.JPG, img02.JPG, img03.JPG, etc. Do NOT use random filenames.

- The FIRST image (img01.JPG) is the reference — it must be captured BEFORE any load is applied.

- Continue capturing until fracture. Post-fracture images can help identify the fracture zone.

| Parameter | Recommended Value | Reason |
| --- | --- | --- |
| Image format | TIFF or high-quality JPG (>90%) | Compression artifacts corrupt DIC |
| Resolution | Minimum 10 megapixels | More pixels = better strain resolution |
| Bit depth | 8-bit minimum, 16-bit preferred | Higher bit depth = better contrast |
| Frame rate | 1 image per load step | Too many images wastes storage; too few misses events |
| Reference image | Before any load | Must be undeformed state |

# 4. MATLAB Online Setup

## 4.1 Accessing MATLAB Online

- Open a web browser and go to: matlab.mathworks.com

- Log in with your MathWorks account (use your IIT Kharagpur institutional email for free access).

- Click 'Open MATLAB Online' to launch the environment.

- The environment has three panels: File browser (left), Editor (centre), Command Window (bottom).

## 4.2 Uploading Images

- In the left panel (MATLAB Drive), click the Upload button.

- Select all 78 images from your local computer.

- Wait for upload to complete. This may take several minutes for large image sets.

- Verify images are visible in the file browser.

- Run this command to verify: ls

⚠ NOTE: MATLAB Online has a storage limit. If you have more than 500 images, upload them in batches or use MATLAB Drive desktop sync app.

## 4.3 Verifying Toolboxes

Run the following command in the Command Window to verify required toolboxes are available:

ver

Confirm these toolboxes appear in the list:

- Image Processing Toolbox

- Statistics and Machine Learning Toolbox

## 4.4 Uploading the DIC Code

- Upload the file dic_main.m to MATLAB Drive using the Upload button.

- Double-click dic_main.m to open it in the editor.

- Do NOT rename the file. MATLAB requires the filename to match the main function name.

# 5. Configuring the DIC Code

Before running the code, you must set the correct parameters in the USER SETTINGS section at the top of dic_main.m. Open the file and locate the section marked USER SETTINGS.

## 5.1 Required Settings

### 5.1.1 File Paths

IMAGE_FOLDER   = '/MATLAB Drive';         % folder containing your images

IMAGE_PATTERN  = 'img*.JPG';              % filename pattern

RESULTS_FOLDER = '/MATLAB Drive/dic_results';  % output folder

⚠ NOTE: IMAGE_PATTERN must match your actual filenames. If your files are named DSC_0001.JPG, use 'DSC_*.JPG'. If named frame001.jpg, use 'frame*.jpg'.

### 5.1.2 Region of Interest (ROI)

ROI = [x1, y1, x2, y2];   % pixel coordinates of gauge section

The ROI defines the gauge section — the narrow speckled area between the two grips. To find the correct coordinates:

- Open img01.JPG in any image viewer.

- Note the pixel coordinates of the top-left corner of the speckle region (x1, y1).

- Note the pixel coordinates of the bottom-right corner (x2, y2).

- Enter these four values in the ROI setting.

⚠ NOTE: In Microsoft Paint, hover the cursor over the image to see pixel coordinates at the bottom of the screen. In MATLAB, use impixelinfo or ginput to interactively select points.

### 5.1.3 DIC Parameters

| Parameter | Default Value | Description | When to Change |
| --- | --- | --- | --- |
| SUBSET_SIZE | 29 | Size of correlation window in pixels (must be odd) | Increase if speckles are large; decrease if gauge is thin |
| STEP_SIZE | 5 | Grid spacing in pixels between measurement points | Decrease for finer strain maps; increases computation time |
| MAX_SHIFT | 40 | Maximum expected displacement in pixels between frames | Increase if large deformations between frames |
| STRAIN_WINDOW | 5 | Window size for LSQ strain calculation (grid points) | Decrease to see localized strain; increase for smoother maps |
| STRAIN_SMOOTH | 1.2 | Gaussian smoothing applied to strain fields | Decrease for sharper maps; increase for smoother |
| MIN_CORR | 0.70 | Minimum ZNCC value — below this, point is masked | Increase to 0.85 to reject more uncertain points |
| REF_GRIP_COLS | 3 | Number of grid columns used as fixed reference | Increase if left grip edge is noisy |

### 5.1.4 Physical Scale (Optional)

GAUGE_LENGTH_MM = [];   % Leave empty if unknown

GAUGE_LENGTH_MM = 5.0;  % Set to actual gauge length in mm if known

If you know the physical gauge length in mm, set this value. The code will then display displacement in mm in addition to pixels on the summary plot.

# 6. Running the Code

## 6.1 How to Run

- Open dic_main.m in the MATLAB editor.

- Verify all settings in the USER SETTINGS section are correct.

- Click the green Run button at the top of the editor, or press F5.

- Alternatively, type the filename in the Command Window: dic_main

## 6.2 What Happens During Execution

The code processes each image in sequence. For each frame you will see a line printed in the Command Window:

Frame 001/077  img02.JPG       ZNCC=0.9878  maxU=+0.23px  exx=+0.020%

| Output | Meaning | Good Range |
| --- | --- | --- |
| Frame 001/077 | Current frame being processed | — |
| img02.JPG | Filename of deformed image | — |
| ZNCC=0.9878 | Mean correlation coefficient | > 0.95 is excellent; < 0.80 is poor |
| maxU=+0.23px | Maximum horizontal displacement relative to left grip | Increases with loading |
| exx=+0.020% | Mean axial strain across gauge | Increases with loading |
| nu=0.391 | Apparent Poisson ratio (shown when reliable) | 0.25–0.45 for metals |

## 6.3 Processing Time

Expected processing time on MATLAB Online:

- 78 images × 1210 grid points ≈ 20–40 minutes

- Do not close the browser tab during processing

- MATLAB Online may timeout after long idle periods — keep the window active

⚠ NOTE: If processing is too slow, increase STEP_SIZE from 5 to 8 or 10. This reduces grid density but speeds up computation significantly.

## 6.4 Output Files

All results are saved to the RESULTS_FOLDER. After completion you will find:

| File | Description |
| --- | --- |
| frame_001.png to frame_077.png | Full-field displacement and strain maps for each frame |
| data_001.mat to data_077.mat | Raw displacement and strain arrays (for further analysis) |
| summary.png | 4-panel summary: axial strain, transverse strain, elongation, Poisson ratio |

# 7. Interpreting the Results

## 7.1 Frame Plots

Each frame_XXX.png contains 8 panels arranged in 4 rows:

| Panel | What it shows | What to look for |
| --- | --- | --- |
| ROI + Grid | Reference image with measurement grid overlay | Green dots = valid points; Red dots = masked/bad points |
| ZNCC Correlation | Correlation quality map | Should be uniformly green (>0.95); yellow/red areas indicate poor tracking |
| U displacement | Horizontal displacement relative to left grip | Should show smooth gradient from 0 (left) to maximum (right) |
| V displacement | Vertical displacement relative to left grip | Should be near zero for pure tensile loading |
| Von Mises strain | Combined strain measure | Should increase uniformly; hot spots indicate strain concentration |
| Axial strain exx | Strain in loading direction | Should be positive and relatively uniform across gauge |
| Transverse strain eyy | Strain perpendicular to loading | Should be negative (Poisson contraction) |
| Shear strain exy | Shear component | Should be near zero for ideal tensile loading |

## 7.2 Summary Plot

The summary.png shows the evolution of key parameters across all frames:

- Axial Strain: Should rise monotonically during loading, then drop/become unreliable after fracture.

- Transverse Strain: Should be negative throughout. Deep negative values in the necking zone are expected.

- Gauge Elongation: Should follow a classic tensile test loading curve shape.

- Poisson Ratio: Should be consistent in the elastic region. Values should cluster around the material's true Poisson ratio.

## 7.3 Identifying Key Events

| Event | How to identify in results |
| --- | --- |
| Elastic loading | Linear increase in exx; consistent Poisson ratio; ZNCC > 0.97 |
| Yield point | Poisson ratio begins to rise above 0.5; exx rate changes |
| Necking onset | Local exx concentration visible in one region; Poisson ratio > 0.5 |
| Fracture | ZNCC drops suddenly below 0.80; displacement field becomes chaotic; masked points increase rapidly |
| Post-fracture | Elongation decreases as specimen springs back; strain values unreliable |

# 8. Validating the Results

Always validate your DIC results before reporting them. Here are the recommended validation steps in order of importance.

## 8.1 Rigid Body Test (Self-Consistency Check)

Run DIC on two identical images (reference vs reference). The result should show zero displacement and zero strain everywhere. Any non-zero value represents the measurement noise floor.

% In MATLAB Command Window:

% Copy img01.JPG to a second file and run DIC on them

% All displacements should be < 0.1 px

% All strains should be < 0.001

## 8.2 Strain Consistency Check

For a uniform gauge section under uniaxial tension:

Expected exx = Max elongation (px) / Gauge length (px)

Example: 50 px / 623 px = 8.0%

Your measured mean exx should match this within ± 1–2%.

## 8.3 Poisson Ratio Check

Compare your measured Poisson ratio against the known value for your material:

| Material | Expected Poisson Ratio |
| --- | --- |
| Aluminium alloys | 0.33 |
| Mild steel | 0.28–0.30 |
| Stainless steel | 0.28–0.31 |
| Copper | 0.34 |
| Brass | 0.34 |
| Titanium | 0.34 |
| Polymers (PMMA, PC) | 0.35–0.40 |

⚠ NOTE: If your Poisson ratio is significantly different from the expected value, check: (1) whether the ROI includes grip regions, (2) whether the specimen material is correctly identified, (3) whether out-of-plane motion is occurring.

## 8.4 Machine Data Comparison (Gold Standard)

If load-displacement data is available from the testing machine, compare the engineering strain from DIC with the extensometer reading from the machine. In the elastic region they should match within 5–10%.

# 9. Do's and Don'ts

## 9.1 During Image Acquisition

| Do | Don't |
| --- | --- |
| Use matte white base coat + matte black speckles | Use glossy or metallic paint |
| Keep camera completely fixed throughout the test | Touch or adjust camera after reference image is taken |
| Use consistent, diffuse lighting | Use autofocus or auto white balance |
| Name images sequentially (img01, img02, ...) | Use random or unsorted filenames |
| Capture reference image before any load is applied | Apply any preload before taking the reference image |
| Use high image quality settings (low compression) | Use high JPEG compression |
| Ensure speckle dots are 3–5 pixels in size | Use too large or too small speckles |

## 9.2 During Code Configuration

| Do | Don't |
| --- | --- |
| Set ROI to gauge section only (between grips) | Include grip regions or machine hardware in ROI |
| Verify image filenames match IMAGE_PATTERN | Assume default pattern works for all cases |
| Use SUBSET_SIZE that fits within ROI height with margin for MAX_SHIFT | Use SUBSET_SIZE larger than half the ROI height |
| Increase MAX_SHIFT if large deformations are expected | Use MAX_SHIFT that is too small — displacement will be capped |
| Check terminal output for ZNCC values during processing | Ignore warnings and errors during processing |

## 9.3 During Result Interpretation

| Do | Don't |
| --- | --- |
| Validate results using rigid body test before reporting | Report results without any validation |
| Mask frames where ZNCC < 0.80 (post-fracture) | Report strain values from low-correlation frames as real data |
| Report displacement as relative (grip-referenced) | Describe displacement as absolute without clarification |
| Compare Poisson ratio with known material value | Accept physically impossible Poisson ratios (e.g. < 0 or > 0.5) without investigation |
| Save .mat data files for further analysis | Rely only on PNG images — raw data may be needed later |

# 10. Troubleshooting Common Problems

| Problem | Likely Cause | Solution |
| --- | --- | --- |
| No images found error | IMAGE_PATTERN does not match filenames | Check exact filenames with ls command; adjust IMAGE_PATTERN |
| ZNCC < 0.80 from start | Poor speckle pattern or bad lighting | Check image quality; verify speckle contrast is high |
| Strain maps show noise / alternating patches | SUBSET_SIZE too small relative to speckle size | Increase SUBSET_SIZE to 41 or 51 |
| Displacement capped at exact value of MAX_SHIFT x 2 | MAX_SHIFT too small for actual deformation | Increase MAX_SHIFT; check displacement magnitude in intermediate frames |
| Poisson ratio = 0 or near zero | ROI includes non-deforming grip regions | Re-select ROI to include only gauge section |
| Rank deficient warning in strain calculation | Too few valid points in strain window at edges | Increase STRAIN_WINDOW or reduce outlier rejection threshold |
| Code runs for > 1 hour | STEP_SIZE too small or MAX_SHIFT too large | Increase STEP_SIZE to 8–10; reduce MAX_SHIFT if possible |
| Frame plots appear black (dark background) | MATLAB Online dark theme affecting export | Ensure InvertHardcopy is set to off in figure properties |
| Summary plot shows extreme Poisson ratio values | Post-fracture frames included in Poisson calculation | Increase MIN_CORR to exclude low-quality frames |
| V displacement shows large gradient top to bottom | Specimen rotating out of plane during loading | Improve gripping; note this as a source of error in report |

# 11. Quick Parameter Reference

Use this table when deciding how to adjust parameters for different experimental conditions:

| Situation | Recommended Parameters |
| --- | --- |
| Thin specimen gauge section (< 150px tall) | SUBSET_SIZE=21, MAX_SHIFT=15, STEP_SIZE=4 |
| Standard specimen (150–300px tall) | SUBSET_SIZE=29, MAX_SHIFT=25, STEP_SIZE=5 |
| Wide specimen (> 300px tall) | SUBSET_SIZE=41, MAX_SHIFT=40, STEP_SIZE=8 |
| Large deformation expected (> 10%) | MAX_SHIFT=50, MIN_CORR=0.70 |
| Want finer strain maps | STEP_SIZE=3, STRAIN_WINDOW=3 |
| Want smoother strain maps | STEP_SIZE=8, STRAIN_WINDOW=7, STRAIN_SMOOTH=2.0 |
| Very noisy speckle pattern | OUTLIER_NSIGMA=2.0, STRAIN_SMOOTH=2.0 |
| Very clean images, high resolution | SUBSET_SIZE=21, STEP_SIZE=3, STRAIN_SMOOTH=0.8 |

# 12. Complete Workflow Summary

Follow these steps in order for a successful DIC analysis:

- Prepare specimen: Sand, clean, apply white base coat, then black speckle pattern. Verify 3–5 px speckle size.

- Set up camera: Mount rigidly, perpendicular to specimen. Fix focus, aperture, ISO, white balance. Disable autofocus.

- Capture reference image: Before any load is applied. Name it img01.JPG.

- Run tensile test: Capture sequential images at regular load/displacement intervals until fracture.

- Upload to MATLAB Online: Upload all images and dic_main.m to MATLAB Drive.

- Configure settings: Set IMAGE_FOLDER, IMAGE_PATTERN, RESULTS_FOLDER, and ROI. Verify DIC parameters.

- Run the code: Press F5 or click Run. Monitor ZNCC values in the terminal output.

- Check results: Open frame plots and summary.png. Verify displacement gradients and strain maps look physically reasonable.

- Validate: Perform rigid body test, check Poisson ratio, compare with machine data if available.

- Report results: Include full-field strain maps, summary plots, Poisson ratio, fracture strain, and necking frame.

End of Standard Operating Procedure

GRISHMA Project | KRITI Initiative | IIT Kharagpur | 2026